## Slide 1: Figures for ASC2016

## Slide 2
Cross sectional view
Sapphire
Not mounted at the time of this test
Permanent magnet
YBCO
Arm
Cryogenic
stepping
motor
Top view
Three grippers hold the rotor magnet.
Temperature sensor
Heater
Gripper1
Gripper2
Gripper3

## Slide 4
Trotor
Tg1,2,3
The grippers held a rotor.
Linear fit
Exponential fit

## Slide 5
Distance 65/3 mm
Thickness 13mm
R = 60mm, 100 degs
  C = 2pi R x 100/360 = 104.7 mm
A = 104.7mm x 13mm
L = 21.7 mm
A/L = 62.7 mm = 6.27 cm
9-0.85 = 8.15 W/cm (for 15K-6K)
Thus, 8.15 x 6.27 = 51.1 W
51.1W/9 K = 5.68 W/K
13mm

## Slide 6
D=384mm
The spin down is measured by using the optical encoder and the Hall sensor is also mounted between the rotor magnet and the YBCO stator. The entire unit is placed in the Styrofoam box with LN2.
Hall sensor
Optical encoder
and chopper

## Slide 7
Spin down measurements at the room temperature with LN2
Model the spin down as
Hysteresis loss
Eddy current
Air friction
The both data and fit are shown.
Time [sec]
0
500
1000
1500
2000
2500
Frequency [Hz]
0.0
0.1
0.2
0.3
0.4
0.5
0.6
0.7
0.8

## Slide 8
Magnetic Field [kG]
Arbitary Unit
Magnetic Field [kG]
Time [sec]
0
0.5
1.0
1.5
2.0
2.5
3.0
0
2.80
2.85
2.90
2.95
3.00
3.00
2.95
2.90
2.85
2.80
2.75
6000
5000
4000
3000
2000
1000
0
One period of rotation

## Slide 9
Magnetic Field [kG]
0
0.5
1.0
1.5
2.0
2.5
3.0
3.00
2.95
2.90
2.85
2.80
2.75
One period of rotation
Time [sec]
ΔB

## Slide 10
One period of
rotation

## Slide 11
One period of
rotation

## Slide 12: Spindown による発熱量計算
P = τω = Iαω , I : イナーシャ , α : 加速度 , ω : 回転速度
I = ½ × M × (Rin^2 + Rout^2) , Rin = 384mm, Rout = 452mm
α (a0) = 5.1e-4 [s^-2] (h=6mm) , α (a0) = 5.7e-3 [s^-2]
ω = 2π (f = 1Hzを仮定)
[M = 3kg リング型 (磁石のみ)の場合]
h = 6mm ) P = (math.pow(384e-3,2) + math.pow(452e-3,2)) * 1/2 * 3 * 2 * math.pi * 5.1e-4 = 1.69mW
h = 3mm ) P = (math.pow(384e-3,2) + math.pow(452e-3,2)) * 1/2 * 3 * 2 * math.pi * 5.7e-3 = 18.9mW
[M = 28kg ディスク型の場合]
ローター重量 21.5kg×1.3(マージン)
(内訳)サファイア： 17kg、 軸受け磁石： 3.4kg、 駆動モーター部： 1.1kg
h = 6mm ) P = math.pow(452e-3,2) * 1/2 * (3 + 21.5*1.3) * 2 * math.pi * 5.1e-4 = 10.1 mW
h = 3mm ) P = math.pow(452e-3,2) * 1/2 * (3 + 21.5*1.3) * 2 * math.pi * 5.7e-3 = 113.2 mW